Mach-zehnder modulators
Mach-zehnder modulators
Theory and Application
Vince Baker
Drexel University

---
Mach-zehnder modulators
Mach-zehnder modulators
- Electro-optic modulators that impress a low-frequency (0-100 GHz) as an amplitude modulation on an optical carrier
- Commonly used in telecommunications industry for wideband data transfer over optical fiber
- Works on electro-optic effect: an applied field causes a change in the index of refraction of a material
Amplitude-modulated output signal
Source laser
Electro-optic material
Input signal

---
Modulated data
Modulated data
Operating region

---
Electro-optic effect (linear)
Electro-optic effect (linear)
- Pockels effect: index of refraction is linear in electric field
- Index of refraction/relative permittivity related to susceptibility of material
- Total phase shift is a function of index of refraction and length of path
- Various tradeoffs between L, d and V determine operating parameters
L
d
E = V/d
V

---
Modulator types
Modulator types
- Discrete: LiNbO3 is the dominant material, >100 GHz bandwidth possible
- Integrated: demonstrated on silicon with lower bandwidth and performance (~10 GHz)
Discrete modulator from EOSpace
“High speed silicon Mach-Zehnder modulator”, L. Liao, D. Samara-Rubio, M. Morse, A. Liu, D. Hodge, Optics Express Vol. 13 No. 8, 18 April 2005

---
indicatrix
indicatrix

---
Indicatrix
Indicatrix
Electro-optic effect described by the electro-optic tensor:
Applied electric field changes the indicatrix shape

---
Lithium niobate structure
Lithium niobate structure
- Lacks inversion symmetry (not centrally symmetric), otherwise the field due to nearby molecules would be 0 (Jackson pp 160-161)
- Symmetry class 3M (three-fold rotational symmetry) leads to electro-optic tensor of the form:

---
Determining electro-optic properties of materials
Determining electro-optic properties of materials
- Material characterization is largely experimental
- Some recent work using density functional theory to determine band structure and optical properties
The imaginary part of from experimental measurements (solid black line) and increasingly accurate calculations (dashed lines) for optical frequencies
“Linear and Nonlinear Optical Response of LiNbO3 Calculated From First Principles”, A. Riefer, S. Sanna, A. Gavrilenko, W. Schmidt, IEEE TRANSACTIONS ON ULTRASONICS, FERROELECTRICS, AND FREQUENCY CONTROL, VOL. 59, NO. 9, SEPTEMBER 2012